## Slide 1: Collaboration with Perugia/Glasgow
Kieran Craig

## Slide 2: Bonding in Perugia
Different HCB procedure is used in Perugia/Virgo to that used by Glasgow/LIGO
Rahul and I learned the procedure used in Perugia from Helios and Flavio
We bonded small pieces of silica and sapphire as practice (silica – 5mm/10mm diameter, sapphire – 5mm diameter)
We also bonded one ear-sized piece to practice bonding larger samples

## Slide 3: Bonding procedures
Virgo HCB Procedure | LIGO HCB Procedure
Cleaning: All pieces submerged in piranha solution (1:3 mixture of H2O2, H2SO4) Bonding surfaces wiped with Isoprop. Bonding surfaces wiped with DI water and blow dried (2x) Bonding solution: KOH salt added to water (1:80 mass ratio) Lots of bonding solution added to the bonding surface, enough to overflow from the sides. Attach second piece. More solution added regularly to the edges until a change in surface tension observed Then water glass solution added | Cleaning: Rinse samples with D.I. Water Clean samples with Cerium Oxide (2x) Clean samples with sodium bicarb. (2x) Rinse samples with DI Water Rinse samples with Methanol Bonding solution: 2ml sodium silicate 12ml DI water Mix, centrifuge, filter with medical filter Apply one drop of bonding solution to one bonding surface, attach second piece

## Slide 5: Bonding small pieces – 5mm and 10mm diameter

## Slide 6: Ear bonding – front view

## Slide 7: Ear bonding – side view

## Slide 8: Ear bonding – back view

## Slide 9: HCB Bonding
Interesting to note the differences, however KAGRA must use the LIGO style bonding
  Surface of sapphire parts usually not flat enough to use Virgo style bonding
LIGO style HCB has a more involved cleaning process, but the bonding process itself is less complicated

## Slide 10: KAGRA mirror box
Great progress made with KAGRA mirror box
The box has been made, with all pieces appropriate for the Prototype mass fabricated (several pieces need to be changed for use with the real KAGRA mirrors)
Box is now in Japan, ready for cleaning, assembly and testing

## Slide 11: KAGRA mirror box

## Slide 12: KAGRA mirror box front panel

## Slide 13: KAGRA mirror box inside

## Slide 14: KAGRA mirror box inside - shelves

## Slide 16: Jig to lift mirror into box

## Slide 17: Discussions at Glasgow
The wire clamps used at the marionette, IM and recoil masses should be improved
Cylinders could be changed to triangular prisms – sapphire pieces used for this purpose in advanced LIGO
  This gives clear definition of break-off point
  In such a case, ANSYS would need to be used to calculate stress in the system to compare with breaking stress of wires
CuBe wires can be fixed to the same length by measuring the violin modes using a guitar pickup and tuning head
Perugia suggested using current system to fix wire length, but then use additional clamps to lock everything down

## Slide 18: Discussions at Glasgow
Does the 1/300 tilt cause problems? Tilt redistributes stress in suspensions. Kazuhiro said that the sapphire fibers should be ok, but how about the CuBe wires? They hold twice the load and are thinner
How do we clean the mirror before bonding? Inside the box or before inserting into the box?
  My idea is to clean it while we are holding it with the jig used to insert the mirror into the box

## Slide 19: Discussions at Glasgow
Marielle will come to Japan to help with bonding, but can only come for one week
  When is best? Should be there when we are doing the cleaning/bonding of sapphire parts, but schedule should be fixed
Also possible for Giles to come to Japan for one week to collaborate on suspensions

## Slide 20: KAGRA HCB (rough) schedule
Prototype box arrived is in Japan
  Cleaning/assembly this week.
Box test using metal ears + mass TBD
  Should measure metal mass/ears using 3D coordinate measurement system before bonding (glue) tests
  Should be repeated several times to test reproducibility of ear placement (sapphire parts can only be bonded once!)
Testing with metal parts should be done this month

## Slide 21: KAGRA HCB (rough) Schedule
Helios will be in Japan during July/August
If necessary, further discussion using metal parts can be done at the start of this time
Sapphire parts will be bonded during Helios’ visit, and the prototype sapphire suspension will begin construction
Must consult KAGRA schedule – when do we expect to be bonding KAGRA ears? (this will be after coating)

## Slide 22: To do:
KAGRA mirror box testing w/ metal parts
Clean room setup for bonding of prototype sapphire parts
3D coordinate measurement system in cleanroom
  LIGO uses Romer arm, but expensive (10^6 JPY)
Fabrication of jig to hold mirror to insert into box (may also be used during cleaning the mirror flats)
Coordinate with mirror subgroup w.r.t. mirror storage, transport, etc.