## Slide 1: Thermal Noise in Opto-Mechanical Systems
Ronny Nawrodt
Workshop, Jena 07/2015

## Slide 2: Noise on different scales
[Kessler et al. Nature Photonics 2012]
[Schließer et al. Nature Physics 2008]
[LIGO Hanford]
laser stabilization
micro /nano resonators
GW detection
µm
cm
km

## Slide 3: Overview
limitations to 2nd generation of GW detectors
thermal noise and materials in opto-mechanical systems
towards a 3rd generation GW observatory – the Einstein Telescope
summary

## Slide 4: Limitations in the second generation

## Slide 5: Improving the sensitivity
low thermal noise material
improved/longer suspensions
low thermal noise material
bigger test masses
higher laser power

## Slide 6: Improving the sensitivity
suspended optics
transmissive and reflective components
schematic view of a Michelson-based iGWD

## Slide 7: Improving the sensitivity
low noise material
  novel materials for optics and suspensions
  (crystalline instead of
  amorphous media)
  cryogenic operational temperature
high laser power
  use of high power lasers
  thermal compensation of beam distortion in transmissive components
  use of non-classical light

## Slide 8: Thermal noise and materials in opto-mechanical systems

## Slide 9: Thermal noise in opto-mechanical systems
What is thermal noise?
fluctuation that couples into the read-out of the system
e.g. optical read-out  only fluctuation at the read-out spot of interest

## Slide 10: Thermal noise in opto-mechanical systems
2 types of thermal noise originating from
  fluctuations of thermal energy kBT
   Brownian noise
  fluctuations of temperature DT
   coupling into the read-out by means of material parameters (dL/dT, dn/dT, etc.)

## Slide 11: Fluctuation-Dissipation-Theorem
macroscopic
mode
microscopic
modes
heat bath
loss f
dissipation
fluctuations / noise
large dissipation  large noise

## Slide 12: Fluctuation-Dissipation-Theorem
simple systems:
Z(w) obtained from equation of motion
What about large systems, e.g. macroscopical optics with 1025 atoms and individual coupling/damping of atoms?
 approach fails due to complexity
with mechanical impedance

## Slide 13: Fluctuation-Dissipation-Theorem
general solution by means of direct approach by Y. Levin (1998)
applying a pressure with force F0 and spatial distribution of read-out beam to surface of optics  deformation energy density u(x,y,z)
Brownian thermal noise is given by
low noise operation: minimize u(x,y,z)  f(x,y,z)
with

## Slide 14: What is the mechanical loss?
s
 = DL/L
relaxation of stress due to microscopical reordering  hysteretic effect  phase lag between deformation e and strain s is called mechanical loss or internal friction

## Slide 15: What is the mechanical loss?
mechanical loss / internal friction measured by ring-down technique
time
amplitude

## Slide 16: What is the mechanical loss?
unique setup developed within the SFB TR7 to study
  bulk materials
  coated materials (dielectric, gratings, etc.)
  bonded materials
wide parameter range
  (2K) 5K – 300K
  up to 500 kHz
  vibrations detectable down to sub nm
  large sample volume
many international collaborations

## Slide 17: Comparison of bulk materials
Sx ~ T  f
candidate materials:
sapphire
silicon

## Slide 18: Study of defects in optical materials
What causes different losses in chemical identical materials?
What is the origin of loss peaks? Which is the optimum operational temperature?
Notes: Bitte hier nur Quarz und Fused Silica drin lassen und ggf. Achsen anpassen. Temperaturschritte 3, 10, 30, 100, 300 K

## Slide 19: Study of defects in optical materials
example: crystalline quartz to calibrate investigations
z-axis
mechanical loss
temperature (K)
12 kHz

## Slide 20: Study of coating materials
HR coating applied to the front of the test mass to form a mirror
mechanical loss of coatings critical  dominating noise source
u(x,y,z)  f(x,y,z)

## Slide 21: Study of coating materials
detailed study of coatings
  deposition technique
  heat treatments
  co-doping (implantation)
  alternative coatings (e.g. crystalline materials, gratings)
4 µm

## Slide 22: Study of jointing techniques
crystalline materials cannot be welded as amorphous ones
detailed study of jointing techniques (hydroxide catalysis bonds, indium, etc.)

## Slide 23: Study of indium bonding
unbonded sample
bonded sample
indium bond
Notes: Englische Beschriftung der Achsen, 25K oder 50K Schritte auf T-Achse.

## Slide 24: Novel terms of thermal noise
free carriers cause change in refractive index  noise
parts of system operated at thermal non-equilibrium  treatment still true?
thermal noise of grating structures
Khalili etalons / cavities
…

## Slide 25: Other properties of the materials
mechanical loss and thermal noise is only 50% of the story
other parameters:
  thermal properties
  optical properties
  mechanical properties
  machining, polishing, coating
  availability (size, purity, …)

## Slide 26: Heat extraction through crystalline materials
expected laser power at mirrors ~ MW
heat removal only through suspension
possible  crystalline fibers needed

## Slide 27: Heat extraction through crystalline materials
detailed study of thermal conductivity (polishing, purity, bonds, …)
Comparison of different surfaces
Comparison of different bonds

## Slide 28: Optical properties of silicon
optical absorption
  little known by 2010 about silicon absorption (especially at cryogenic temperatures)
  project C9 „Optical properties of silicon-based optics“ born
band gap of silicon at 1.12 eV (@ 300K)
  absorption @ 1064nm ~ 80%
  change to 1550nm needed
  residual absorption beyond the gap
  needs measurements
valence band
conduction band
phonons
electronic absorption of silicon

## Slide 29: Optical properties of silicon
room temperature
cryogenic temperature
4 ppm/cm
demonstrated
level at low temperatures ~ level
at room temperature
4 ppm sensitivity demonstrated

## Slide 30: Optical properties of silicon
thermo-refractive index
  temperatur fluctuations in transmissive optics cause phase change due to dn/dT  unknown parameter

## Slide 31: Optical properties of silicon
birefringence
  stress (impurities, gravity) can induce birefringence
  level Dn ~ 10-7
  imaging setup developed to „see“
  birefringence

## Slide 32: Mechanical properties of silicon
Young‘s modulus influences deformation energy and this thermal noise
Breaking strength tests of Si, Si-Sapphire, Sapphire-Sapphire samples
Orientation |  |  | 
Normal energy | 0.77 | 0.52 | 0.3
Shear energy | 0.23 | 0.40 | 0.45
without defects | 1 | 0.91 | 0.88
with defects | 3.05 | 4.48 | 4.92
Orientation |  |  | 
Normal energy | 0.77 | 0.52 | 0.3
Shear energy | 0.23 | 0.40 | 0.45
 | 1 | 0.91 | 0.88
 | 3.05 | 4.48 | 4.92

## Slide 33: The einstein telescope
Towards a 3rd generation gravitational wave observatory

## Slide 34: Sensitivity goals
cryogenics
high laser power
?

## Slide 35: Design study for the Einstein Telescope
many people of the SFB TR7 involved
lots of results (squeezing, material issues, thermal noise modelling) of SFB groups went into the conceptual design
to be found on www.et-gw.eu

## Slide 36: Xylophone design of the Einstein Telescope
10-20K, 18kW, 1550nm
300K, 3MW, 1064nm

## Slide 37: Use of squeezed light
reduced laser power needed for
same sensitivity
less thermal load in the system
(thermal lensing)
key feature of ET-HF
Squeezing

## Slide 38: The Einstein Telescope as a GW Observatory
Combination of several detectors in one site  correlation can be used to reduce technical noises

## Slide 39: Materials for the Einstein Telescope
450 mm
300 mm
Source: http://www.iisb.fraunhofer.de/content/dam/iisb/de/images/geschaeftsfelder/halbleiterfertigungsgeraete_und_methoden/gadest_2011/
Source: www.pvatepla.com
1m
size available
purity under development

## Slide 40: Low thermal noise suspensions
300K detector: low thermal noise
good seismic isolation of test mass
low temperature detector:
low thermal noise
good seismic isolation of test mass
high thermal conductivity to remove heat
?

## Slide 41: Low thermal noise suspensions

## Slide 42: Investigation of possible sites
seismic studies throughout Europe

## Slide 43: How to built an underground facility?
NIKHEF

## Slide 44: The Einstein Telescope – An artist view
artist view of ET
vertical vs. horizontal access

## Slide 45: From 0th to 3rd generation
KAGRA

## Slide 46: Sensitivity of the Einstein Telescope (BNS)
GRB050509B
Einstein Telescope
aLIGO AdV KAGRA
1ST GENERATION
[G. Cagnoli, LMA)

## Slide 47: Summary and conclusions

## Slide 48: Summary and Conclusions
2nd generation of GW detectors will provide first direct observation of GWs
3rd generation of GW detectors will be needed to do GW astronomy
materials and cryogenic operation will play cruicial role for 3rd generation detectors